SPECIFICATION – 119 Sto Decocoat Floor Finish

Acrylic-based, Colored Quartz Aggregate Finish

SECTION 09985

DECOCOAT FLOOR FINISH

# PART 1 - GENERAL

## SUMMARY

##### Provide decorative quartz aggregate finish system for horizontal concrete substrates.

##### Related Sections:  Other specification sections which relate directly to the work of this section include the following:

###### Section 03300, Cast-In-Place Concrete

###### Section 09980, Clearcoat Sealer.

## SUBMITTALS

##### Product Data:  Submit manufacturer's product data and installation instructions for each material and product used.  Include manufacturer's Material Safety Data Sheets.

## REFERENCES

##### ASTM D 570, Water Absorption

##### ASTM D 5020,Surface Abrasion

##### ASTM G 23, Accelerated Weathering

##### ASTM C 297, Modified, Adhesion

## QUALITY ASSURANCE

##### Manufacturer's Qualifications: The manufacturer shall be a company with at least five years experience and regularly engaged in the manufacture and marketing of products specified herein.  The manufacturer shall have an ISO 9001 certified quality system.

##### Installer's Qualifications: The contractor shall be qualified to perform the work specified by reason of experience.

##### DELIVERY, STORAGE AND HANDLING

##### Deliver products in original packaging, labeled with product identification, manufacturer, batch number and shelf life.

##### Store products in a dry area with temperature maintained between 50 and 85 degrees F (10 and 29 degrees C).  Protect from direct sunlight.  Protect from freezing.

##### Handle products in accordance with manufacturer's printed recommendations.

# PART 2 - PRODUCTS

### MATERIALS

##### Surface Primer: Acrylic-based primer compatible with and tinted to match quartz aggregate finish.  Comply with the following:

###### Manufacturer:  801 Sto Primer, as manufactured by Sto Corp., PO Box 44609, Atlanta, GA, 30336-5609; telephone 404-346-3666.

##### Quartz Aggregate finish: Acrylic-based colored quartz aggregate finish. Comply with the following.

###### Manufacturer: 119 Sto Decocoat, as manufactured by Sto Corp.

###### Performance and Physical Properties: Meet or exceed the following values at 73 degrees F (23 degrees C) and 50 percent relative humidity:

Working Time: 30 – 45 minutes.

Water Absorption: 8%, 24-hour immersion, ASTM D 570

Surface Abrasion: 0.01 percent weight loss, ASTM D 5020 (Taber H-38 wheel)

Accelerated Weathering: No deleterious effects after 2000 hours, ASTM G 23.

Adhesion to Primed Concrete Surface: > 125 psi (0.9 MPa), ASTM C 297, Modified.

# PART 3 - EXECUTION

#### INSTALLATION OF STO DECOCOAT

##### Examine substrates and conditions under which materials will be installed.  Do not proceed with installation until unsatisfactory conditions are corrected.

##### Coordinate installation with adjacent work to ensure proper sequence of construction.  Protect adjacent areas and landscaping from contact due to mixing and handling of materials.

###### Surface Preparation: Clean surface to be treated using a low pressure (<1000 psi (<6.9 MPa)) water wash, and allow to dry completely.

##### Mixing:

###### Use material undiluted.

###### Mix with a drill and paddle to a uniform consistency immediately before use.

##### Application:

###### Apply when ambient and surface temperatures are 50 degrees F (10 degrees C) and rising and will remain above 50 degrees F (10 degrees C) for 24 hours.

###### Do not apply in freezing conditions, during precipitation,or during cool, damp weather.

###### Apply primer using a low-pressure sprayer, roller, or brush.

###### Allow primer to dry (normally 2 to 4 hours at 70-75 degrees F (21-24 degrees C)).

###### Apply Sto Decocoat using a hopper sprayer or trowel.

Spray sufficient material to completely cover primer.  Spray applications may be left as sprayed or troweled smooth immediately after spraying.  Trowel finishing must be completed within the material working time, which varies with temperature and humidity.

Trowel Decocoat to a thickness approximately 1.5 times the aggregate size (1.5 mm).

###### Allow to dry a minimum 48 hours.  Cool or damp weather requires extended drying.

###### Apply two coats of Sto Clear Coat Sealer in accordance with Section 09980.

###### Do not apply to areas exposed to vehicular traffic, heavy pedestrian traffic, ponding or puddling water, food waste, oil, grease, or harsh chemicals. Do not apply to shower floors.  Apply only to properly sloped areas with light to moderate foot traffic.

###### Periodic re-sealing is required as a function of traffic and weather exposure.

##### Cleaning:  Clean tools and equipment with water immediately after use.  If material has cured, remove using mechanical methods that will not damage surrounding construction.

END OF SECTION

ATTENTION

Sto products are intended for use by qualified professional contractors, not consumers, as a component of a larger construction assembly as specified by a qualified design professional, general contractor or builder.  They should be installed in accordance with those specifications and Sto’s instructions.  Sto Corp. disclaims all, and assumes no, liability for on-site inspections, for its products applied improperly, or by unqualified persons or entities, or as part of an improperly designed or constructed building, for the nonperformance of adjacent building components or assemblies, or for other construction activities beyond Sto’s control.  Improper use of Sto products or use as part of an improperly designed or constructed larger assembly or building may result in serious damage to Sto products, and to the structure of the building or its components.  STO CORP. DISCLAIMS ALL WARRANTIES EXPRESS OR IMPLIED EXCEPT FOR EXPLICIT LIMITED WRITTEN WARRANTIES ISSUED TO AND ACCEPTED BY BUILDING OWNERS IN ACCORDANCE WITH STO’S WARRANTY PROGRAMS WHICH ARE SUBJECT TO CHANGE FROM TIME TO TIME.  For the fullest, most current information on proper application, clean-up, mixing and other specifications and warranties, cautions and disclaimers, please refer to the Sto Corp. website, www.stocorp.com.