Sto Corp.

3800 Camp Creek Pkwy.

Building 1400, Suite 120

Atlanta, GA  30331

Tel:	   404-346-3666

Toll Free:    800-221-2397

Fax:            404-346-3119

Web:           www.stocorp.com

STO GUIDE SPECIFICATION

SPECIFICATION CR241/CR242 Sto Watertight Coat with CR218 Repair Mesh

Polymer Modified Cementitious, Trowel Applied Membrane Waterproofing

SECTION 07165

CEMENTITIOUS WATERPROOFING

# PART 1 - GENERAL

## SUMMARY

##### Provide acrylic based waterproofing for existing substrate.

##### Related Sections:  Other specification sections which relate directly to the work of this section include the following:

###### Section 03300, Cast-In-Place Concrete.

## SUBMITTALS

##### Product Data:  Submit manufacturer's product data and installation instructions for each material and product used.  Include manufacturer's Material Safety Data Sheets.

## REFERENCES

##### ASTM D 4541, Pull-Off Strength of Coatings

##### ASTM D 412, Tensile Strength and Elongation

##### ASTM D 522, Mandrel Bend Flexibility

##### ASTM D 4060, Abrasion Resistance Using the Taber Abraser

##### ASTM D 570, Water Absorption

##### ASTM D E96, Water Vapor Transmission

##### DIN 1048, German Industry Norm for Testing Hardened Concrete

##### ICRI Guide 03732, Specifying Concrete Surface Preparation for Sealers, Coatings, and Polymer Overlays

## QUALITY ASSURANCE

##### Manufacturer's Qualifications: The manufacturer shall be a company with at least five years experience and regularly engaged in the manufacture and marketing of products specified herein.  The manufacturer shall have an ISO 9001 certified quality system.

## Installer's Qualifications: The contractor shall be qualified to perform the work specified by reason of experience DELIVERY, STORAGE AND HANDLING

##### Deliver products in original packaging, labeled with product identification, manufacturer, batch number and shelf life.

##### Store products in a dry area with temperature maintained between 50 and 85 degrees F (10 and 29.5 degrees C).  Protect from direct sunlight.  Protect from freezing.

##### Handle products in accordance with manufacturer's printed recommendations.

## DELIVERY, STORAGE AND HANDLING

##### Deliver products in original packaging, labeled with product identification, manufacturer, batch number and shelf life.

##### Store products in a dry area with temperature maintained between 50 and 85 degrees F (10 and 29.5 degrees C).  Protect from direct sunlight.  Protect from freezing.

##### Handle products in accordance with manufacturer's printed recommendations.

# PART 2 - PRODUCTS

### MATERIALS

##### Cementitious waterproofing: Two-component flexible membrane, containing portland cement and an acrylic emulsion with fine fibers.  Comply with the following:

###### CR241/CR242 Sto Watertight Coat as manufactured by Sto Corp., PO Box 44609, Atlanta, GA, 30336-5609; telephone 404-346-3666.

###### Performance and Physical Properties:  Meet or exceed the following values for material cured at 73 degrees F (23 degrees C) and 50 percent relative humidity:

Working Time:  30- 90 minutes.

Adhesion to Concrete: 150 psi (1.05 MPa) at 7 days, ASTM D4541.

Tensile Strength:  470 psi (3.24 MPa) without mesh, 3800 psi (26.2 MPa) with mesh, ASTM D412

Flexibility Mandrel Bend:  passes 1/8” @ 77 degrees F (25 degrees C) at 28 days, ASTM D522

Abrasion Resistance: 0.9% weight loss at 3,000 cycles, 1.5% at 6,000 cycles, ASTM D4060, Taber CS-10 Wheel.

Water Absorption: 4.5% at 24 –hr immersion,  ASTM D570

Waterproofing (hydrostatic pressure resistance) Greater than 101.5 psi (0.7 MPa) over concrete substrate, DIN 1048.

Vapor Permeability:  3.85 US Perms (2.2x10-7 g/Pa∙m∙s), ASTM E96 Procedure B

Color:  Concrete gray (CR 241), white (CR 242)

Combustibility:  Non-combustible, both before and after use.

# B.	Reinforcing Mesh: Polymer coated glass fiber interlaced reinforcing mesh, compatible with cementitious waterproofing material. Comply with the following:

###### CR218 Sto Repair Mesh as furnished by Sto Corp.

# PART 3 - EXECUTION

#### INSTALLATION OF CEMENTITIOUS WATERPROOFING

##### Examine substrates and conditions under which materials will be installed.  Do not proceed with installation until unsatisfactory conditions are corrected.

##### Coordinate installation with adjacent work to ensure proper sequence of construction.  Protect adjacent areas and landscaping from contact due to mixing and handling of materials.

##### Surface Preparation:  Comply with manufacturer's printed instructions and the following.

###### Remove loose and deteriorated materials using high pressure water- or sand-blasting or mechanical wire brushing.

###### Clean surfaces of bond inhibiting materials including mildew, dust, dirt, laitance and standing water.

###### Surface shall have an ICRI Concrete Surface Profile of CSP 5 or lower.

##### Mixing:  Comply with manufacturer's printed instructions and the following.

###### Precondition components to temperature of 70 plus or minus 5 degrees F (21 plus or minus 2.5 degrees C) prior to mixing.

###### Mix using a mechanical mixer until components are evenly blended to uniform lump-free consistency.  Do not add water.

##### Application:  Comply with manufacturer's printed instructions and the following.

###### Apply when ambient and surface temperatures are 45 degrees F (7.5 degrees C) and rising and are expected to remain above 45 degrees F (7.5 degrees C) for 24 hours following placement.

###### Do not apply in freezing conditions or during precipitation.

###### Comply with manufacturer’s guides for hot and cold weather application.

###### Bridge cracks up to 1/32 inch (0.8 mm) with Sto Repair Mesh embedded in Sto Watertight Coat. Do not bridge cracks greater than 1/32 inch (0.8 mm). Provide alternate repair method for such cracks. Do not bridge expansion, control or isolation joints.  Provide alternate waterproofing treatment.

###### Reinforce monolithic changes in plane—corners, coves, etc.—with Sto Repair Mesh embedded in Sto Watertight Coat minimum 6 inches in each direction.

###### Apply to maximum 1/16 inch (1.6 mm) thickness:

Apply in a single pass with a stainless steel trowel.

Alternatively spray into place and trowel to a 1/16-inch (1.6mm) thickness.

###### If required, embed repair mesh into freshly applied material.  Smooth wrinkles, force down, and cover with cementitious waterproofing material.

###### Allow to dry a minimum of 24 hours before overcoating.

###### Protect from rain until completely dry.

###### Do not overcoat with solvent-based materials.

###### Do not use in lieu of a roofing membrane over occupied space.

###### Do not use as between-the-slab waterproofing.

##### Cleaning:  Remove excess material before material cures.  If material has cured, remove using mechanical methods that will not damage substrate.

END OF SECTION

Copyright 2000 Sto Corporation.  All Rights Reserved.

A copyright license to reproduce this specification is granted to specifying architects and engineers.

ATTENTION

Sto products are intended for use by qualified professional contractors, not consumers, as a component of a larger construction assembly as specified by a qualified design professional, general contractor or builder.  They should be installed in accordance with those specifications and Sto’s instructions.  Sto Corp. disclaims all, and assumes no, liability for on-site inspections, for its products applied improperly, or by unqualified persons or entities, or as part of an improperly designed or constructed building, for the nonperformance of adjacent building components or assemblies, or for other construction activities beyond Sto’s control.  Improper use of Sto products or use as part of an improperly designed or constructed larger assembly or building may result in serious damage to Sto products, and to the structure of the building or its components.  STO CORP. DISCLAIMS ALL WARRANTIES EXPRESS OR IMPLIED EXCEPT FOR EXPLICIT LIMITED WRITTEN WARRANTIES ISSUED TO AND ACCEPTED BY BUILDING OWNERS IN ACCORDANCE WITH STO’S WARRANTY PROGRAMS WHICH ARE SUBJECT TO CHANGE FROM TIME TO TIME.  For the fullest, most current information on proper application, clean-up, mixing and other specifications and warranties, cautions and disclaimers, please refer to the Sto Corp. website, www.stocorp.com.