Project Name:

Project Number:

Section 31 32 19

Specification for Woven Wicking Geotextile Used in Roadway Stabilization

- GENERAL

  - SECTION INCLUDES

    - Woven Geotextile to provide moisture management, stabilization, separation and reinforcement for the aggregate subbase or base of an unpaved or paved roadway.

# RELATED SECTIONS

    - Section 02 50 00 - Site Remediation

    - Section 01 89 13 - Site Preparation Performance Requirements

    - Section 31 00 00 - Earthwork

    - Section 32 10 00 - Bases, Ballasts, Pavements, and Appurtenances

# UNIT PRICES

    - Method of Measurement: By the square yard (or square meter - as indicated in contract documents) including seams, overlaps, and wastage.

    - Basis of Payment: By the square yard (or square meter - as indicated in contract documents) installed.

# REFERENCES

    - AASHTO Standards:

      - GTX-22-01 Technical Committee Work Plan for Evaluation of Geotextile and Facility Audits

      - R 50-09 Standard Practice for Geosynthetic Reinforcement of the Aggregate Base Course of Flexible Pavement Structures

      - M288 - Geotextile Specification for Highway Applications

    - American Society for Testing and Materials (ASTM):

      - D422 - Standard Test Method for Particle-Size Analysis of Soils

      - D4354 - Practice for Sampling of Geosynthetics for Testing

      - D4355 - Test Method for Deterioration of Geotextiles from Exposure to Ultraviolet Light and Water (Xenon-Arc Type Apparatus)

      - D4439 - Terminology for Geotextiles

      - D4491 - Test Methods for Water Permeability of Geotextiles by Permittivity

      - D4595 - Test Method for Tensile Properties of Geotextiles by the Wide- Width Strip Method

      - D4751 - Test Method for Determining Apparent Opening Size of a Geotextile

      - D4759 - Practice for Determining the Specification Conformance of

      - Geosynthetics

      - D4873 - Guide for Identification, Storage, and Handling of Geotextiles

      - D6241 - Standard Test Method for the Static Puncture Strength of Geotextiles and Geotextile-Related Products Using a 50-mm Probe

      - D6706 - Standard Test Method for Measuring Geosynthetic Pullout Resistance in Soil

      - D6767 - Standard Test Method for Pore Size Characteristics of Geotextiles by Capillary Flow Test

      - C1559 – Standard Test Method for Determining Wicking

    - Federal Highway Administration (FHWA) - Geosynthetic Design and Construction Guidelines, Publication No. FHWA HI-95-038, April 1998.

    - Geosynthetic Materials Association (GMA) White Paper I, May 1991 & White Paper II, June 2000.

    - Geosynthetic Accreditation Institute (GAI) - Laboratory Accreditation Program (LAP)

    - International Standards Organization (ISO) - 9001:2015

# DEFINITIONS

    - Minimum Average Roll Value (MARV): Property value calculated as typical minus two standard deviations. Statistically, it yields a 97.7 percent degree of confidence that any sample taken during quality assurance testing will exceed value reported.

# SUBMITTALS

    - Submit the following:

      - Certification: The contractor shall provide to the Engineer a certificate stating the name of the manufacturer, manufacturing location(s), product name, style number, and chemical composition of the filaments or yarns and other pertinent information to fully describe the geotextile. The Certification shall state that the furnished geotextile meets MARV requirements of the specification as evaluated under the Manufacturer's quality control program. The Certification shall be attested to by a person having legal authority to bind the Manufacturer. Certifications from Private Label distributors will not be accepted.

      - Any alternate product must be submitted following section 2.2.1 Alternate Material Submittal requirements.

# QUALITY ASSURANCE

    - Manufacturer Qualifications:

      - The geotextile Manufacturer shall have all the following credentials:

        - ISO 9001:2015 Quality Management System

        - Geosynthetic Accreditation Institute (GAI) Laboratory Accreditation Program (LAP)

    - The geotextile Manufacturer shall have a GAI-LAP accredited laboratory at the location of production capable of performing the ASTM tests as outlined in the specification.

# DELIVERY, STORAGE, AND HANDLING

    - Geotextile labeling, shipment, and storage shall follow ASTM D4873. Product labels shall be color-coded to specifically identify each product and clearly show the Manufacturer’s name, style name, and roll number. The geotextile shall be labeled directly on the product at an interval not greater than every 5 meters (15 feet) indicating the product name and manufacturing number per NTPEP GTX labeling requirements.

    - Each geotextile roll shall be wrapped with a material that will protect the geotextile from damage due to shipment, water, sunlight, and contaminants.

    - During storage, geotextile rolls shall be elevated off the ground and adequately covered to protect them from the following: site construction damage, precipitation, extended ultraviolet radiation including sunlight, chemicals that are strong acids or strong bases, flames including welding sparks, excess temperatures, and any other environmental conditions that may damage the physical property values of the geotextile.

# PRODUCTS

  - MANUFACTURERS

    - Solmax (TenCate Geosynthetics) 365 South Holland Drive Pendergrass, GA, USA 30567

1-800-685-9990

1-706-693-2226

1-706-693-4400, fax

www.tencategeo.us

# MATERIALS

    - Geotextile:

      - The geotextile shall be woven from super high-tenacity polypropylene yarns in conjunction with wicking yarns with a weave pattern to maximize strength, water flow, soil interaction, wicking capabilities and soil retention. The yarns shall be from high-tenacity long-chain synthetic polymers composed of at least 95 percent by weight of polyolefins or polyamides. They shall form a stable network such that the filaments or yarns retain their dimensional stability relative to each other, including selvages.

      - Approved geotextiles are as follows:

          - MIRAFI H2Ri. Any submitted product other than MIRAFI H2Ri is considered an alternate.

      - The MIRAFI H2Ri has the following Quality Control properties for material verification. The properties in Table 1 shall not be used as equivalent performance and performance verification for alternate materials must be provided per Section 2.2.1. All numeric values in Table 1 except AOS represent MARV in the specified direction. Values for AOS represent maximum measured opening size.

# TABLE 1 – WOVEN WICKING GEOTEXTILE

| Mechanical Properties | Test Method | Unit | Minimum Average Roll Value |  |
| --- | --- | --- | --- | --- |
|  |  |  | MD | CD |
| Wide Width Tensile Strength | ASTM D4595 | lbs/ft (kN/m) | 5280 (77.0) | 5280 (77.0) |
| Wide Width Tensile Strength @ 2% strain | ASTM D4595 | lbs/ft (kN/m) | 480 (7.0) | 1080 (15.8) |
|  |  |  | Maximum Opening Size |  |
| Apparent Opening Size (AOS) | ASTM D4751 | U.S. Sieve (mm) | 40 (0.425) |  |
|  |  |  | Minimum Roll Value |  |
| Permittivity | ASTM D4491 | sec-1 | 0.4 |  |
| Flow Rate | ASTM D4491 | gal/min/ft2 (l/min/m2) | 30 (1222) |  |
|  |  |  | Minimum Test Value |  |
| Pore Size (O50) | ASTM D6767 | microns | 180 |  |
| Pore Size (O60) | ASTM D6767 | microns | 234 |  |
| Pore Size (O95) | ASTM D6767 | microns | 391 |  |
| Wet Front Movement 1 (24 minutes) | ASTM C15592 | inches | 6.0 Vertical direction |  |
| Wet Front Movement 1 (983 minutes) Zero Gradient | ASTM C15592 | inches | 73.3 Horizontal direction |  |

1 ‘STP’: Standard Temperature and Pressure, Tested Value

2 Modified

Refer to Manufacturer’s Installation Guidelines.

    - ALTERNATE MATERIAL SUBMITTAL

- This project has been designed and specified using the MIRAFI® H2Ri geosynthetic, any alternate product must demonstrate equivalent performance to the specified material.

      - Any proposed alternate materials must be submitted to the Engineer a minimum of 15 days prior to the bid date. No alternate materials will be considered after this time.

      - Submittal must include full scale performance testing performed by an independent testing agency that quantifies the structural benefit of the of the geotextile. The benefit must meet or exceed the benefit of the design geotextile under similar conditions. A design including the alternate geotextile must be stamped by a professional engineer in the state where the project is located and submitted for review. Manufacturer’s installation Guidelines shall be provided.

      - One sample of the alternate material with minimum dimensions of 1 foot x 1 foot sample shall be provided.

      - Quality Standards: The contractor shall provide to the Engineer the Manufacturer’s Quality Control Plan along with their current GAI-LAP and ISO 9001:2015 certificates.

      - Alternate product submittals must also include information on five similar projects in size and scope.

# QUALITY CONTROL

    - Manufacturing Quality Control: Testing shall be performed at an on-site laboratory accredited by GAI-LAP for tests required for the geotextile, at frequency meeting or exceeding ASTM D4354.

    - Manufacturer's certifications and testing of quality assurance samples obtained using Procedure B of ASTM D4354. A lot size for conformance or quality assurance sampling shall be the shipment quantity of the given product or a truckload of the given product, whichever is smaller.

# EXECUTION

  - See Manufacturer’s Installation guidelines provided in the submittal.

# END OF SECTION

Mirafi™ is a registered trademark of Nicolon Corporation.	Copyright © 2015 Nicolon Corporation. All Rights Reserved.