SECTION 07 18 13

DECORATIVE PEDESTRIAN TRAFFIC COATINGS

The accompanying guide specification has been prepared by Tremco Incorporated according to principles established in the Project Resource Manual published by The Construction Specifications Institute.  It is provided to assist design professionals, building owners and others in the preparation of a specification section covering installation of decorative pedestrian traffic coatings for concealed building components in critical areas such as those subject to hydrostatic pressure or occupied by personnel, vehicles or equipment.  It may be used in conjunction with most commercially available master specification sections with minor editing as the basis for developing a project specification or an office master specification.

Please contact your nearest Tremco Representative or Tremco Incorporated at 1-800-852-8173 for additional information or design assistance.

THE PRODUCT:  Liquid-applied polyurethane waterproofing coating system designed for concrete and plywood decks subject to pedestrian traffic, meeting ASTM C 957-91 and having UL 790 Class A fire rating on concrete deck surfaces.

1.   The coating system:

a.	Is seamless;

b.	Fully bonds to concrete and plywood substrates both adhesively and mechanically;

c.	Bridges developing cracks up to 1/16" in concrete substrates;

d.	Is suitable for continuous immersion in water;

e.	Can be applied to concrete, masonry, plywood, and metal substrates;

f.	Aesthetic achieved with decorative ceramic-coated aggregates in pre-blended colors affording broad possibilities;

g.	Clear topcoat is aliphatic polyurethane providing outstanding wear resistance.

COORDINATION:  Guide Section 07 18 13 defines requirements of the decorative pedestrian deck waterproofing system itself.  It is important to define certain substrate requirements and requirements of adjacent trades in pertinent other sections of your specification as follows:

1.   Section 03 30 00 - Cast-In-Place Concrete

a.	Concrete finish should be equivalent to one lightly steel troweled followed by a fine hair broom.

b.	Suitable wet-cure method should be used.

c.	Consult ACI & PCA standards for placement of control joints in topping slabs over precast planks.

d.	Drain flanges at coating level should be integrally cast into and flush with concrete deck surfaces that slope to the drains.

2.   Section 05 58 00 - Formed Metal Fabrications

a.	Metal flashings that are substrate to the waterproofing coating system should be minimum 24 gauge aluminum, galvanized or stainless steel.

b.	Set metal flashings in continuous bedding bead of urethane sealant such as Vulkem 116/921, install sealant S-bead between metal laps and mechanically fasten to substrate along leading edges at every 4 inches o.c., staggered linearly, to lay flat without fish mouths.

3.   Section 06 12 00 - Structural Decking

a.	Plywood that is substrate to the waterproofing coating system must be exterior grade minimum 5/8 inch thick with A-side up, fastened with ring-shank nails.

b.	Plywood decking must be blocked under every joint unless it is tongue-and-groove minimum 1-1/8 inch thick.

c.	Deck surfaces should slope to drain.  Deck drains must have flanges at the coating level that are flush with the deck surface.

d.	OSB and particle boards are not suitable substrates.

END OF COVER PAGE(S)

SECTION 07 18 13

DECORATIVE PEDESTRIAN TRAFFIC COATINGS

Before using this Guide Section, fully read the associated cover page(s) for information about its use and important requirements that must appear in other Sections of the Project Manual.  Carefully review this Guide and delete inapplicable text.

Part 1 - GENERAL

1.01	Summary

A.   Section includes:  Provide a complete, liquid-applied polyurethane, decorative waterproofing coating system designed for decks subject to pedestrian traffic, including all applicable sealants and elastomeric flashings needed to prevent water penetration, where shown on the Drawings and as specified herein.

B.   Related work:

1.	Documents affecting Work of this Section include, but are not necessarily limited to, General Conditions, Supplementary Conditions, and Sections in Division 1 of these Specifications.

1.02	Submittals

A.   Comply with pertinent provisions of Section 01 33 00.

B.   Product data:

1.	Materials list of items proposed to be provided under this Section;

2.	Manufacturer's specifications and other data needed to prove compliance with the specified requirements;

3.	Shop Drawings or catalog illustrations in sufficient detail to show installation and interface of the work of this Section with the work of adjacent trades;

4.	Manufacturer's current recommended installation procedures which, when reviewed by Architect, will become the basis for accepting or rejecting actual installation procedures used on the Work;

5.	Written documentation of applicator's qualifications, including reference projects of similar scope and complexity, with current phone contacts of architects and owners for verification.

1.03	Quality Assurance

A.   Use adequate numbers of skilled workmen thoroughly trained and experienced in the necessary crafts and completely familiar with the specified requirements and methods needed for proper performance of the work of this Section.

B.   Applicator qualifications:

1.	Applicator shall have at least three years experience in installing materials of types specified and shall have successfully completed at least three projects of similar scope and complexity.

2.	Applicator shall designate a single individual as project foreman who shall be on site at all times during installation.

C.   Convene a pre-installation job-site conference four weeks prior to commencing work of this Section:

1.	Secure attendance by Architect, Contractor, applicator, and authorized representatives of the coating system manufacturer and interfacing trades.

2.	Examine Drawings and Specifications affecting work of this Section, verify all conditions, review installation procedures, and coordinate scheduling with interfacing portions of the Work.

1.04	Delivery, Storage and Handling

A.   Deliver materials to job site in manufacturer's unopened containers with all labels intact and legible at time of use.

B.   Maintain the products in accord with manufacturer's recommendations with proper precautions to ensure fitness of material when installed.

C.   Comply with pertinent provisions of Section 01 66 00.

1.05	Substrate Conditions

A.   General:

1.	Provide applicator with surfaces that are broom clean, dry, sound and free of voids, bug holes, rock pockets, honeycombs, protrusions, excessive roughness, foreign matter, frost, ice and other contaminants which may inhibit application or performance of the waterproofing coating system.

2.	Using suitable abrasive methods, remove residue of form release, curing compound, chemical retarders and other surface treatments, laitance, mortar smear, saw cutting residue, mill scale, rust, loose material and other contaminants from concrete, masonry and ferrous metal surfaces to receive the work of this Section.

B.   Concrete:  Where work of this Section will be applied to concrete, provide surfaces that are smooth with finish equal to one that is light steel troweled followed by a fine hair broom.

C.   Plywood:  Where work of this Section will be applied to plywood, provide exterior grade plywood, 5/8" thick minimum, with A-side up, fastened with ring-shank nails.

D.   Decks:

1.	Slope deck surfaces to drains that have flanges at coating level which are flush with deck surfaces.

2.	Rigidly install pipe, vents and other surface protrusions, properly flash them, and cover to prevent entry of coating materials.

E.   Metal flashings:  Where metal flashings are substrate to waterproofing coating, set the flashings in continuous bedding bead of urethane sealant; install sealant S-bead between metal laps and mechanically fasten to substrate along leading edges at every 4" on center, staggered linearly, to lay flat without fish mouths.

F.   Joints:  Configuration shall be consistent with this Section and with all other requirements of the Contract Documents.

1.06	Warranty

A.   Deliver to the Architect signed copies of the following written warranties against defective materials and workmanship for a period of five years following date of completion.  Warrant that installed waterproofing coating system shall be free of defects including adhesive failure, cohesive failure, weathering deficiencies and waterproofing failure resulting from substrate cracking up to 1/16 inch.

1.	Manufacturer's standard warranty covering materials;

2.	Applicator's standard warranty covering workmanship.

Part 2 - PRODUCTS

2.01	General

A.	Provide a complete liquid applied polyurethane waterproofing coating system having the following minimum attributes:

1.	System designed for waterproofing decks subject to pedestrian traffic;

2.	Complying with ASTM C 957-91 and having a Class A fire rating on concrete substrates.

3.	Finish color to be provided by decorative manufactured color quartz aggregate in color blend selected by Architect.

4.	Acceptable products:

a.   Vulkem 951NF-Clear

b.   or prior approved equal

2.02	Accessories

A.   Primer:  As recommended by coating system manufacturer.

B.   Joint backing:  Closed-cell, polyethylene rod as recommended by coating manufacturer.

C.   Decorative aggregate:  40-50 mesh manufactured ceramic coated quartz granules, factory blended and packaged, approved by coating manufacturer.

D.   Sealant:

1.	Dymeric 240FC

2.	Vulkem 116 with catalyst

3.	THC 900-901

4.	Vulkem 45 SSL

5.	or prior approved equal

2.03	Other Materials

A.   Provide other materials, not specifically described but required for a complete and proper installation, as selected by the Contractor and approved by the coating system manufacturer as compatible, subject to review of the Architect.

Part 3 - EXECUTION

3.01	Surface Conditions

A.   Coordinate as required with other trades to assure proper and adequate provision in the work of those trades for interface with the work of this Section.

B.   Applicator shall examine the areas and conditions under which work of this Section will be performed.

1.	Verify conformance with manufacturer's requirements;

2.	Report unsatisfactory conditions in writing to the Architect;

3.	Do not proceed until unsatisfactory conditions are corrected.

3.02	Preparation

A.   Surface preparation and detailing procedures to be in accord with waterproofing coating system manufacturer's instructions and recommendations except where more stringent requirements are indicated.

B.   Clean all deck surfaces to receive coating system in accord with manufacturer's instructions; vacuum clean or blow clean with oil-free compressed air all surfaces to receive sealants, detailing materials or coatings immediately prior to installation.

C.   Rout, clean, prepare and detail surface cracks in accord with manufacturer's instructions; install backer rod where required.

D.   Clean metal surfaces to bright metal by wire brushing or mechanical etching; scuff-sand lead flashing and plastic surfaces.

E.   Prime surfaces in accord with manufacturer's instructions.

F.   Install 1/4" diameter backer rod into corner of all horizontal-to-vertical junctures subject to movement and cover with 1" detail cant of approved sealant; install 1" detail cants at projections, curbs and other horizontal-to-vertical junctures.

G.   Install detail coats, joint and crack treatments, and liquid flashings in accord with manufacturer's instructions.

H.   Allow detail applications to cure in accord with manufacturer's instructions prior to general application of coating.

3.03	Application

A.   Install waterproofing coating system in accord with manufacturer's recommendations and instructions as applies to the Work except where more stringent requirements are indicated.

1.	Grid deck surfaces to assure proper coverage rates and verify coating wet-film mil thickness with gauges as work progresses.

2.	Retain empty product containers during course of work to aid in determining whether completed coating system complies with manufacturers average thickness requirements.

B.   Verify proper dry condition of substrate using method recommended by coating system manufacturer; perform adhesion checks prior to general application of coating system using field adhesion test method recommended by manufacturer.

C.   Mask off adjoining surfaces not to receive coating system.

D.   Wipe clean all detail coats with white rags wetted with Xylene solvent; do not saturate detail coat.

E.   Apply coating base coat uniformly and allow to cure in accord with manufacturer's instructions.

F.   Feather edge when entire area cannot be completed in one day;  clean area 6" wide along edge of coating with Xylene solvent on clean white rags prior to startup on next working day;  use interlaminary primer per manufacturer's instructions as needed;  overlap existing work by 6" with new work.

G.   Apply coating system finish coat evenly in accord with manufacturer's instructions.  Immediately broadcast decorative aggregate to flood surface of wet material.  Allow to cure per manufacturer's instructions.

H.   Vacuum up loose aggregate.  Apply even application of coating system clear finish coat and immediately broadcast decorative aggregate to flood surface of wet material.  Allow to cure per manufacturer's instructions.  Do not reuse vacuumed aggregate unless passed through a window screen to remove lumps and contaminants.

I.    Vacuum up loose aggregate and apply final lock coat application of coating system clear finish coat at rate recommended by manufacturer.  Allow to cure per manufacturer's instructions.

3.04	Protection and Clean-Up

A.   Promptly remove primer or coating material from adjacent surfaces with MEK, Toluene or Xylene; leave work area in vacuum clean condition.

B.   Allow completed Work to cure 24 hours before opening to pedestrian traffic.

END OF SECTION