The accompanying guide specification has been prepared by Tremco Incorporated according to principles established in the Manual of Practice published by The Construction Specifications Institute.  It is provided to assist design professionals, building owners and others in the preparation of a specification section covering removal of concrete deck overlay material, repair to concrete surfaces and installation of new waterproofing coating system for decks subject to vehicular traffic.  It may be used in conjunction with most commercially available master specification sections with minor editing as the basis for developing a project specification or an office master specification.

This specification guide is provided in two parts as follows:

*	Cover Page (file 07186cvr.* on diskette):  Conveys important requirements that should appear in other pertinent Sections of the project Specifications.

*	Section 07186 (file 07186spc.* on diskette):  A guide specification that may be used as is or modified as you wish.

Please contact your nearest Tremco Architectural Services Representative or Tremco Incorporated (800) 852-8173 for additional copies, information on available electronic formats or design assistance.

THE PRODUCT:  Liquid-applied polyurethane waterproofing coating system designed for decks subject to vehicular traffic, meeting ASTM C 957-91 and having UL 790 Class A fire rating on concrete deck surfaces.  The coating waterproofs to protect occupied areas underneath and protects concrete substrates from damaging effects of deicing salts, chemicals, gasoline, oils and anti-freeze.

1.	The waterproofing coating system:

a.	Is seamless;

b.	Fully bonds to substrates both adhesively and mechanically;

c.	Bridges developing cracks up to 1/16" in concrete and masonry substrates;

d.	Can be applied to concrete, masonry, plywood and metal substrates;

e.	Can be used in a broad variety of exposed conditions on parking decks, vehicular drive aisles, vehicular ramps and on roof decks such as beneath window washing equipment.

f.	Is part of a single-source system of products that includes waterproofing joint sealants and factory-molded seals for wide joints providing a complete system approach and single-source manufacturer responsibility.

COORDINATION:  Section 07186 defines requirements for the liquid applied polyurethane waterproofing coating system itself, along with repair to the concrete surface.  It is important to define certain substrate requirements and requirements of adjacent trades in pertinent other sections of your specification as follows:

1.	Section 03300 - Cast-in-place concrete:

a.	Concrete that is substrate to the coating system should have a finish equal to light steel troweling followed by a fine hair broom.

b.	An appropriate wet curing procedure should be used on the concrete.

c.	Control joints in the concrete, if required, should be in accordance with pertinent ACI and PCA standards.

d.	Drain flanges at coating level should be integrally cast into, and be flush with, concrete deck surfaces that slope to drain.

2.	Section 04200 - Concrete unit masonry:

a.	Mortar joints should be tooled at surfaces to receive this waterproofing system.

3.	Section 05800 - Expansion control:

a.	Tremco produces the Vulkem 255 FM Premolded Joint Seals for covering and waterproofing wide expansion joints in parking decks, stadiums, plazas and similar large concrete structures. Vulkem 255 is compatible with the waterproofing coating system and permit single-source manufacturer responsibility in a total system approach.

4.	Section 07600 - Flashing and sheet metal:

a.	Metal flashings that are substrate to the waterproofing coating system should be a minimum of 24 gage aluminum, galvanized, or stainless steel.

b.	Set metal flashings in continuous bedding bead of urethane sealant such as Vulkem116/921, installing sealant S-bead between metal laps and mechanically fastening to substrate along leading edges at every 4" on center, staggered linearly, to lay flat and without fishmouths.

EDITING OF GUIDE SECTION 07186: Paragraph 2.1A of the accompanying guide section 07186 calls for a wear balanced system that incorporates the heavy duty vehicular system in areas of heavier wear.  Paragraphs 3.2 B, C and D of the accompanying guide Section 07186 provide for a general removal of existing overlaying materials from concrete substrates and provide surface repairs to the concrete that is exposed.  Your attention is called to these paragraphs that you may review and edit them to adequately reflect your project conditions.  We recommend that you consult with engineering disciplines and such industry organizations as ACI (American Concrete Institute, 810-848-3700) and ICRI (International Concrete Repair Institute, 703-450-0116) for repairs of a structural nature to concrete components.

END OF COVER PAGE(s)

Before using this Guide Section, fully read the associated cover page(s) (on diskette as file 07186cvr.*) for information about its use and important requirements that must appear in other Sections of the Project Manual.  Carefully review this Guide and delete inapplicable text.

PART 1	GENERAL

1.01	SUMMARY

A.	Section includes:

1.	Removal and disposal of existing overlay materials as indicated, repair and preparation of substrates, and installation of a complete polyurethane waterproofing coating system.

2.	Work includes all applicable sealants and elastomeric flashings needed to ensure a complete waterproof and weathertight system for deck, ramp and raised curb surfaces at locations indicated.

B.	Related work:

1.	Documents affecting work of this Section include, but are not necessarily limited to, General Conditions, Supplementary Conditions, and Sections in Division 1 of these Specifications.

1.02	SUBMITTALS

A.	Comply with pertinent provisions of Section 01330.

B.	Product data:

1.	Materials list of items proposed to be provided under this Section;

2.	Manufacturer's specifications and other data needed to prove compliance with the specified requirements;

3.	Shop Drawings or catalog illustrations in sufficient detail to show installation and interface of the work of this Section with the work of adjacent trades;

4.	Manufacturer's current recommended installation procedures which, when reviewed by Architect, will become the basis for accepting or rejecting actual installation procedures used on the Work;

5.	Coating system manufacturer's affidavit that manufactured polymer-modified concrete repair materials are verified compatible with coating system;

6.	Written documentation of applicator's qualifications, including reference projects of similar scope and complexity, with current phone contacts of architects and owners for verification.

1.03	QUALITY ASSURANCE

A.	Use adequate numbers of skilled workmen thoroughly trained and experienced in the necessary crafts and completely familiar with the specified requirements and methods needed for proper performance of the work of this Section.

B.	Applicator qualifications:

1.	Applicator shall have at least three years experience in installing materials of types specified and shall have successfully completed at least three projects of similar scope and complexity.

2.	Applicator shall designate a single individual as project foreman who shall be on site at all times during installation.

C.	Convene a pre-installation job-site conference four weeks prior to commencing work of this Section:

1.	Secure attendance by Architect, Contractor, applicator, and authorized representatives of the coating system manufacturer and interfacing trades.

2.	Examine Drawings and Specifications affecting work of this Section, verify all conditions, review installation procedures, and coordinate scheduling with interfacing portions of the Work.

1.04	DELIVERY, STORAGE AND HANDLING

A.	Deliver materials to job site in manufacturer's unopened containers with all labels intact and legible at time of use.

B.	Maintain the products in accord with manufacturer's recommendations with proper precautions to ensure fitness of material when installed.

C.	Comply with pertinent provisions of Section 01660.

1.05	SUBSTRATE CONDITIONS

A.	General:

1.	Provide applicator with surfaces that are broom clean, dry, sound and free of voids, bugholes, rockpockets, honeycombs, protrusions, excessive roughness, foreign matter, frost, ice and other contaminants which may inhibit application or performance of the waterproofing coating system.

2.	Using suitable abrasive methods, remove residue of form release, curing compound, chemical retarders and other surface treatments, mortar smear, sawcutting residue, mill scale, rust, loose material and other contaminants from concrete, masonry and ferrous metal surfaces to receive the work of this Section.

B.	Concrete:  Where work of this Section will be applied to concrete, provide surfaces that are smooth with finish equal to one that is light steel troweled followed by a fine hair broom.

C.	Decks:

1.	Slope deck surfaces to drains that have flanges at coating level which are flush with deck surfaces.

2.	Rigidly install pipe, vents and other surface protrusions, properly flash them, and cover to prevent entry of coating materials.

D.	Metal flashings:  Where metal flashings are substrate to waterproofing coating, set the flashings in continuous bedding bead of urethane sealant; install sealant S-bead between metal laps and mechanically fasten to substrate along leading edges at every 4" on center, staggered linearly, to lay flat without fishmouths.

E.	Joints:  Configuration shall be consistent with this Section and with all other requirements of the Contract Documents.

1.06	WARRANTY

A.	Deliver to the Architect signed copies of the following written warranties against defective materials and workmanship for a period of two years following date of completion.  Warrant that installed waterproof coating system shall be free of defects including adhesive failure, cohesive failure, weathering deficiencies and waterproofing failure resulting from substrate cracking up to 1/16 inch.

1.	Manufacturer's standard warranty covering materials;

2.	Applicator's standard warranty covering workmanship.

PART 2	PRODUCTS

2.01	GENERAL

A.	Provide a complete liquid applied polyurethane waterproofing coating having the following minimum attributes:

1.	System designed for concrete decks subject to vehicular traffic;

2.	Complying with ASTM C957-91 and having a Class A fire rating on concrete surfaces;

3.	Install manufacturer's standard-duty vehicular traffic deck system on parking areas from curbs to end of striped parking stalls and raised curb areas indicated;

4.	Install manufacturer's heavy-duty vehicular traffic deck system on ramps, drive aisles and turn areas indicated;

5.	Color to be selected by Architect from manufacturer's standard color range.

6.	Acceptable products:

a.	Vulkem 350SLorR/345/346

- Vulkem 350SLorR/345/346NF

- Vulkem 360NF/950NF/950NF (uv concealed areas)

- Vulkem 360NF/950NF/951NF (uv exposed areas)

c.	or prior approved equal

2.02	ACCESSORIES

A.	Primer:  As recommended by coating system manufacturer.

B.	Joint backing:  Closed-cell, polyethylene rod as recommended by coating manufacturer.

C.	Aggregate:  20-30 mesh silica sand; local aggregate approved by coating manufacturer

D.	Sealant:

1.	Dymeric  240/240FC

- Vulkem 227

- THC 900-901

3.	or prior approved equal

2.03	OTHER MATERIALS

A.	Provide other materials, not specifically described but required for a complete and proper installation, as selected by the Contractor and approved by the coating system manufacturer as compatible, subject to review of the Architect.

PART 3	EXECUTION

3.01	SURFACE CONDITIONS

A.	Coordinate as required with other trades to assure proper and adequate provision in the work of those trades for interface with the work of this Section.

B.	Applicator shall examine the areas and conditions under which work of this Section will be performed.

1.	Verify conformance with manufacturer's requirements;

2.	Report unsatisfactory conditions in writing to the Architect;

3.	Do not proceed until unsatisfactory conditions are corrected.

3.02	PREPARATION

A.	Surface preparation and detailing procedures to be in accord with waterproof coating system manufacturer's instructions and recommendations except where more stringent requirements are indicated.

B.	Remove existing overlay materials and residue.

1.	Use mechanical means approved by Architect to expose sound, bondable surface of structural concrete base slab;

2.	Remove high ridges and reach low spots for total removal;

3.	Ensure resulting surface profile conforms with requirements of subsequent topping treatment.

C.	Remove to sound concrete all spalled, delaminated, deteriorated or otherwise deficient concrete from structural concrete surfaces to receive polymer-modified cementitious repair mortar;  vacuum clean or blow clean with oil-free compressed air to assure all loose particles have been removed.

D.	Repair concrete and correct slope using polymer-modified cementitious repair mortars mixed, installed and cured according to manufacturers instructions.

1.	Finish to profile required for coating system;

2.	Do not use liquid curing compounds.

E.	Abrade concrete surfaces by light bead-blast to remove laitance and provide surface texture resembling 100 grit sandpaper.

F.	Clean all deck surfaces to receive coating system in accord with manufacturer's instructions;  vacuum clean or blow clean with oil-free compressed air all surfaces to receive sealants, detailing materials or coatings immediately prior to installation.

G.	Rout, clean, prepare and detail surface cracks in accord with manufacturer's instructions;  install backer rod where required.

H.	Clean metal surfaces to bright metal by wire brushing or mechanical etching;  scuff-sand lead flashing and plastic surfaces.

I.	Prime surfaces in accord with manufacturer's instructions.

J.	Install 1/4" diameter backer rod into corner of all horizontal-to-vertical junctures subject to movement and cover with 1" detail cant of approved sealant;  install 1" detail cants at projections, curbs and other horizontal-to-vertical junctures.

K.	Install detail coats, joint and crack treatments, and liquid flashings in accord with manufacturer's instructions.

L.	Allow detail applications to cure in accord with manufacturer's instructions prior to general application of coating.

3.03	APPLICATION

A.	Install waterproof coating system in accord with manufacturer's recommendations and instructions as applies to the Work except where more stringent requirements are indicated.

1.	Grid deck surfaces to assure proper coverage rates and verify coating wet-film mil thickness with gauges as work progresses.

2.	Retain empty product containers during course of work to aid in determining whether completed coating system complies with manufacturers average thickness requirements.

B.	Verify proper dry condition of substrate using method recommended by coating system manufacturer;  perform adhesion checks prior to general application of coating system using field adhesion test method recommended by manufacturer.

C.	Mask off adjoining surfaces not to receive coating system.

D.	Wipe clean all detail coats with white rags wetted with Xylene solvent;  do not saturate detail coat.

E.	Apply coating base coat uniformly and allow to cure in accord with manufacturer's instructions.

F.	Feather edge when entire area cannot be completed in one day;  clean area 6" wide along edge of coating with Xylene solvent on clean white rags prior to startup on next working day;  use interlaminary primer per manufacturer's instructions as needed;  overlap existing work by 6" with new work.

G.	Mix and apply coating system intermediate wear coats in accord with manufacturer's instructions for wear balance specified; immediately broadcast aggregate into wet material at rate recommended by manufacturer; disperse aggregate through a hopper fed, low pressure air blower in a manner to ensure uniform coverage over entire surface and backroll to evenly distribute and totally encapsulate; allow to cure per manufacturer's instructions.

H.	Apply coating system finish coat in accord with manufacturer's instructions.

3.04	PROTECTION AND CLEAN-UP

A.	Promptly remove primer or coating material from adjacent surfaces with MEK, Toluene or Xylene;  leave work area in broom clean condition.

B.	Allow completed Work to cure 72 hours before opening to vehicular traffic.

END OF SECTION