SECTION 09 29 00

USG DUROCK CEMENT BOARD WITH EDGEGUARD

2.5   CEMENT BOARD

Cementitious Backer Panel <INSERT PANEL DESIGNATION HERE>:

Basis of Design: Subject to compliance with project requirements, the design is based on the following: USG Corporation, LLC, ” USG Durock Cement Board” .

Classification: Cementitious Backer Units: ANSI A118.9, ASTM A108.11 and ASTM C 1325 provide with manufacturer's standard edges.

Thickness: [1/4 inch (6.4 mm)] [1/2 inch (12.7 mm)] [5/8 inch (15.9 mm)] [As indicated].

Board Length: [5 feet (1524 mm)] [8 feet (2438 mm)] [As indicated].

Board Width: [32 inches (813 mm)] [36 inches (914 mm)] [48 inches (1219 mm)] [As indicated].

Mold Resistance: ASTM D 3273, score of 10 as rated according to ASTM D 3274.

Minimum bending radius: 6 feet (1830 mm).

Fastener Requirements:  Provide fasteners of size and type indicated that comply with requirements specified in this Article for material and application.

Screws for Fastening Gypsum Sheathing to Cold-Formed Metal Framing:  DUROCK Brand Steel or USG Sheathing SF steel drill screws [1-1/4 inch] [1-5/8 inch] [2-1/4 inch] with corrosion-resistant coating.

Wood Screws:  DUROCK Brand Wood or USG Sheathing WF screws [1-1/4 inch] [1-5/8 inch] [2-1/4 inch] with corrosion-resistant coating.

Nails:  11-gauge hot-dipped galvanized roofing nails [1-1/2 inch (38 mm)] [1-3/4 inch (44 mm)], 7/16 11 mm inch diameter head.

Installation Requirements:

For steel framing less than 0.0329 inch thick, attach sheathing to comply with ASTM C 1002.

For steel framing from 0.033 to 0.112 inch thick, attach sheathing to comply with ASTM C 954.

Disclaimer:  The USG Product Specifications contained herein are intended for use as product reference material by architects, engineers, other design professionals, contractors, building code officials, or other competent construction industry trade professionals having an interest in the selection, specification and use of products manufactured by the subsidiaries of USG Corporation. The specifications are intended solely as technical support incident to the sale and use of USG products and not intended to be a substitute for the design review and approval of the licensed design professionals for the project.  These materials may be printed and/or transferred electronically solely as needed by the user. Because electronic files can be modified by other parties, without notice or indication of such modifications, modification of USG Product Guide Specifications is the sole responsibility of the Design Professional.