SECTION 09 29 00

USG FIBEROCK® BRAND AQUA-TOUGH™ AR INTERIOR PANELS

PART 2  FIBER REINFORCED INTERIOR GYPSUM BOARD

Fiber Reinforced Interior Gypsum Board ASTM C1278: Standard Classification for Fiber Reinforced Interior Gypsum Panel Products.

Basis of Design: Subject to compliance with project requirements, the design is based on the following: “USG Corporation, Fiberock® Brand Aqua-Tough™ Abuse Resistant Panels Regular and type X Panels”.

Abrasion Resistance; Level 1.

Indentation Resistance; Level 1.

Soft Body Impact Resistance; Level 2.

Hard Body Impact Resistance; Level 1.

UL Type Designation “FRX-G”.

ASTM E84 Surface-Burning Characteristics:

Flame Spread: 5.

Smoke Developed: 0.

Thickness: [½” (12.4 mm )] [5/8” (15.9 mm)].

Length: [8’-0” (2438)] [9’-0” (2743)] [10’-0” (3048)] [12’-0” (3658)].

Widths: 48" (1219).

Weight: [2.4] [3.1] lb./ft2.

Long Edges: Tapered.

Disclaimer:  The USG Product Specifications contained herein are intended for use as product reference material by architects, engineers, other design professionals, contractors, building code officials, or other competent construction industry trade professionals having an interest in the selection, specification and use of products manufactured by the subsidiaries of USG Corporation. The specifications are intended solely as technical support incident to the sale and use of USG products and not intended to be a substitute for the design review and approval of the licensed design professionals for the project.  These materials may be printed and/or transferred electronically solely as needed by the user. Because electronic files can be modified by other parties, without notice or indication of such modifications, modification of USG Product Guide Specifications is the sole responsibility of the Design Professional.