| # General Specification Notes: | # References in blue are general indicators to the specifier. # References in red relate to fire-rated assemblies and/or code related issues, if not applicable, delete. |
| --- | --- |

| SECTION 061600 / 06 16 43 SHEATHING Securock Brand Glass Mat Sheathing |  | Product Specification |
| --- | --- | --- |

- GENERAL

- 1.01	SUMMARY

        - This Section includes the following:

          - Wall Sheathing.

          - Weather-Resistant Sheathing Barriers.

        - Related Sections include the following:

          - Section 018113 – Sustainable Design Requirements.

          - Section 054000 – Cold-Formed Metal Framing.

          - Section 061000 – Rough Carpentry.

- 1.02	REFERENCES

- A.	American Society for Testing and Materials:

- ASTM C 297: Standard Test Method for Flatwise Tensile Strength of Sandwich Constructions

- ASTM C 954: Specification for Steel Drill Screws for the Application of Gypsum Panel Products or Metal Plaster Bases to Steel Studs from 0.033 inch to 0.110 inch in Thickness

- ASTM C 1002:  Standard Specification for Steel Self-Piercing Tapping Screws for the Application of Gypsum Panel Products or Metal Plaster Bases to Wood Studs or Steel Studs.

- ASTM C 1177:  Standard Specification for Glass Mat Gypsum – Substrate for use as Sheathing.

- ASTM C 1280:  Standard Specification for Application of Gypsum Sheathing.

- ASTM C 1396:  Standard Specification for Gypsum Board.

- ASTM D 226:  Standard Specification for Asphalt-Saturated Organic Felt Used in Roofing and Waterproofing.

- ASTM E 84:  Standard Test Method for Surface Burning Characteristics of Building Materials.

- ASTM E 119:  Test Method for Fire Tests of Building Construction and Materials.

- ASTM E 1677:  Standard Specification for an Air Retarder (AR) Material or System for Low-Rise Framed Building Walls.

- B.	Gypsum Association:

- 1.	GA 253:  Recommended Specification for the Application of Gypsum Sheathing.

- 1.03	SUBMITTALS

- A.	General:  Submit in accordance with Section 013300

- B.	Product Data:  Submit manufacturer’s current technical literature for product specified.

- 1.04	QUALITY ASSURANCE

- A.	Fire Resistance Rated Assembly Characteristics:  Provide materials and construction identical to those tested in accordance to ASTM E 119 by an independent testing and inspection agency acceptable to authorities having jurisdiction.

- 1.	Fire Resistance Ratings:  Indicated by design designations from UL Fire Resistance Directory.

- 1.05	DELIVERY, STORAGE, AND HANDLING

- A.	All materials shall be delivered in their original unopened packages and stored in an enclosed shelter providing protection from damage and exposure to the elements.  WARNING:  Store all SECUROCK Brand Glass Mat Sheathing flat.  Panels are heavy and can fall over, causing serious injury or death.  Do not move unless authorized.

- PRODUCTS

- 2.01	WALL SHEATHING

        - Glass Mat Gypsum Sheathing:  ASTM C 1177 gypsum sheathing.

          - Product:  Subject to compliance with requirements, provide SECUROCK Brand Glass Mat Sheathing by United States Gypsum Company.

          - Type and Thickness:  [Regular, 1/2 inch] [Type X, 5/8 inch] thick.

          - Size:  [48 by 96 inches] [48 by 108 inches] [48 by 120 inches] with square edge.

- 2.02	FASTENERS

        - General:  Provide fasteners of size and type indicated that comply with requirements specified in this Article for material and application.

        - Nails:  11-gauge hot-dipped galvanized roofing nails [1-1/2 inch] [1-3/4 inch], 7/16 inch diameter head – (Minimum).

        - Wood Screws:  # 6  [1-1/4 inch] [1-5/8 inch] [2-1/4 inch] with a corrosion-resistance of more than 800 hours per ASTM B117 (Minimum).

        - Screws for Fastening Sheathing to Cold-Formed Metal Framing:  #6  [1-1/4 inch] [1-5/8 inch] [2-1/4 inch] with corrosion-resistance of more than 800 hours per ASTM B117 (Minimum).

          - For steel framing less than 0.0329 inch thick, attach sheathing to comply with ASTM C 1002.

          - For steel framing from 0.033 to 0.112 inch thick, attach sheathing to comply with ASTM C 954.

- 2.03	WEATHER-RESISTANT SHEATHING PAPERS (Weather Resistive Barrier)

        - Building Paper:  ASTM D 226, Type 1 (No. 15 asphalt-saturated organic felt), unperforated.

        - Building Wrap:  ASTM E 1677, Type I air retarder, with flame-spread and smoke-developed indexes of less that 25 and 450, respectively, when tested according to ASTM E 84, UV stabilized and acceptable to authorities having jurisdiction.

          - Products:  Subject to compliance with requirements, provide Tyvek StuccoWrap by DuPont (E. I. du Pont de Nemours and Company).

        - Building-Wrap Tape:  Pressure-sensitive plastic tape recommended by building wrap manufacturer for sealing joints and penetrations in building wrap.

- 2.04	MISCELLANEOUS MATERIALS

        - Sealant For Glass Mat Gypsum Sheathing Board:  Elastomeric, medium-modulus, neutral-curing silicone joint sealant compatible with joint substrates formed by gypsum sheathing and other materials.

        - Sealant for Glass-Mat Gypsum Sheathing Board: Silicone emulsion sealant complying with ASTM C 834, compatible with sheathing tape and sheathing.

        - Sheathing Tape for Glass-Mat Gypsum Sheathing Board:  Self –adhering, glass fiber tape, minimum 2” wide for use with silicone emulsion sealant in sealing joints in glass-mat gypsum sheathing board.

        - Flexible Flashing:  Composite, self-adhesive, flashing product consisting of a pliable, rubberized-asphalt compound, bonded to a high-density, cross-laminated polyethylene film.

        - Primer for Flexible Flashing:  Product recommended by manufacturer of flexible flashing for substrate.

- EXECUTION

- 3.01	INSTALLATION, GENERAL

        - Do not use materials with defects that impair quality of sheathing or pieces that are too small to use with minimum number of joints or optimum joint arrangement.

        - Cut panels at penetrations, edges, and other obstructions of work; fit closely against abutting construction, unless otherwise indicated.

        - Coordinate wall sheathing installation with flashing and joint-sealant installation so these materials are installed in sequence and manner that prevent exterior moisture from passing through completed assembly.

        - Do not bridge building expansion joints; cut and space edges of panels to match spacing of structural support elements.

- 3.03	SHEATHING INSTALLATION

        - Comply with ASTM C 1280, GA-253 and manufacturer's written instructions.

          - Fasten sheathing to wood framing with [nails] [screws].

          - Fasten sheathing to cold-formed metal framing with screws.

          - Install boards with a 3/8-inch gap where non-load-bearing construction abuts structural elements.

          - Install boards with a 1/4-inch gap where they abut masonry or similar materials that might retain moisture, to prevent wicking.

        - Apply fasteners so heads bear tightly against face of sheathing boards but do not cut into facing.

        - Sheathing may be installed with the long dimension of the sheathing either parallel or perpendicular to framing.  Board orientation to be dictated by performance requirements.  Abut ends and/or edges of the boards centered over face of framing members.  Offset board joints by not less than one stud spacing

          - Space fasteners a maximum of  8 inches o.c. and set back a minimum of 3/8 inch from edges and ends of boards.  Adjust spacing of fasteners to meet specific fire or structural performance requirements.

          - For sheathing under stucco cladding, boards may be initially tacked in place with screws if overlying self-furring metal lath is screw-attached through sheathing to studs immediately after sheathing is installed.

- 3.04	WEATHER-RESISTANT SHEATHING PAPER INSTALLATION

        - General:  Cover sheathing with weather-resistant sheathing paper as follows:

          - Cut back barrier 1/2 inch on each side of the break in supporting members at expansion- or control-joint locations.

          - Apply barrier to cover vertical flashing with a minimum 4-inch overlap, unless otherwise indicated.

        - Building Paper:  Apply horizontally with a 2-inch overlap and a 6-inch end lap; fasten to sheathing with galvanized staples or roofing nails.

        - Building Wrap:  Comply with manufacturer's written instructions.

          - Seal seams, edges, fasteners, and penetrations with tape.

          - Extend into jambs of openings and seal corners with tape.

- 3.05	FLEXIBLE FLASHING INSTALLATION

        - Apply flexible flashing where indicated to comply with manufacturers written instructions.

          - Prime substrates as recommended by flashing manufacturer.

          - Lap seams and junctures with other materials at least 4 inches, except that at flashing flanges of other construction, laps need not exceed flange width.

          - Lap flashing over weather-resistant building paper at bottom and sides of openings.

          - Lap weather-resistant building paper over flashing at heads of openings.

          - After flashing has been applied, roll surfaces with a hard rubber or metal roller to ensure that flashing is completely adhered to substrates.

END OF SECTION 061643