SECTION 07 50 00

USG SECUROCK® BRAND GYPSUM FIBER ROOF BOARD

2.2   SUBSTRATE BOARD, USG SECUROCK® GYPSUM FIBER ROOF BOARD

Gypsum Fiber Roof Board ASTM C1278, “Standard Specification for Fiber-Reinforced Gypsum Panel.”

Basis of Design: Subject to compliance with project requirements, the design is based on the following: “USG Securock® Brand Gypsum Fiber Roof Board”.

UL Type Designation “FRX-G”.

ASTM D 3273: Mold Resistance: Score of 10 as rated according to ASTM D 3273.

ASTM E96: [24] [26] [30].

ASTM E84 Surface-Burning Characteristics:

Flame Spread: 5.

Smoke Developed: 0.

ASTM E661 Flute Span-ability: [2 5/8” (66)] [5” (127)] [8” (203)].

ASTM C518 R value: [0.2] [0.3] [0.5] [0.6].

Compressive Strength: 1800 psi.

Thickness: [1/4” (66.4)] [3/8” (9.5)] [1/2” (12.7)] [5/8” (15.9)].

Length: [4’-0” (1219)] [8’-0” (2438)].

Widths: 48" (1219).

Weight: [1.57] [1.96] [2.76] [3.2] lb./ft2.

Bending Radius: [25’-0” (7620)] [30’-0” (9144)].

Long Edges: Square.

Disclaimer:  The USG Product Specifications contained herein are intended for use as product reference material by architects, engineers, other design professionals, contractors, building code officials, or other competent construction industry trade professionals having an interest in the selection, specification and use of products manufactured by the subsidiaries of USG Corporation. The specifications are intended solely as technical support incident to the sale and use of USG products and not intended to be a substitute for the design review and approval of the licensed design professionals for the project.  These materials may be printed and/or transferred electronically solely as needed by the user. Because electronic files can be modified by other parties, without notice or indication of such modifications, modification of USG Product Guide Specifications is the sole responsibility of the Design Professional.