SECTION 092900 – Gypsum Board, 1″ USG Sheetrock® Brand Gypsum Liner Panels®

|  |
| --- |
| **Product Summary:**  |
| * 1" paper-faced liner panels with moisture resistance.
* Double-beveled edges for easy installation.
* Score and snap easily; no special handling required.
* UL Classification as to fire resistance, surface-burning characteristics and non-combustibility.
* Comprehensive product and system testing assures long term performance and safety.
* Achieved GREENGUARD Gold Certification.
* Refer to product submittal sheet WB2278 for more information.
* Contact USG at800.874.4968 for technical questions.
 |

|  |
| --- |
| **Note to Specifiers:**  |
| * This document is not intended to function as a standalone specification. It is intended to assist the specifier in inserting the proper language into the following recommended specification sections:

09 29 00 – GYPSUM BOARD.* For use with any UL design where UL Type SLX panels are listed.
* This light weight product will be produced at all USG gypsum board plants, substantially reducing distances and carbon footprint for transport.
 |

PART 2 –PRODUCTS

* + - 1. GYPSUM SHAFT LINER PANEL
				1. Gypsum Board ASTM C1396/C1396M.

Basis of Design: Subject to compliance with project requirements, the design is based on the following: United States Gypsum Company, LLC, “USG Sheetrock® Brand Shaft Liner Panels.

UL Type Designation “SLX”.

ASTM E136 Non-combustibility: Meets or exceeds criteria.

ASTM E84 Surface-Burning Characteristics:

Flame Spread: 20.

Smoke Developed: 0.

ASTM C473:

Core Hardness: Meets or Exceeds 11 (ASTM C473 B).

Flexural Strength (lbft).

Parallel: Not less than 77.

Perpendicular: Not less than 228.

Thickness: 1 inch (25.4 mm).

Length: [8′-0″ (2440 mm)] [10′-0″ (3050 mm)] [12′-0″ (3660 mm)].

Width: 2’-0″ (609 mm).

Weight: 4 lbs./sq. ft.

Long Edges: Double Beveled.

Disclaimer: The USG Product Specifications contained herein are intended for use as product reference material by architects, engineers, other design professionals, contractors, building code officials, or other competent construction industry trade professionals having an interest in the selection, specification and use of products manufactured by the subsidiaries of USG Corporation. The specifications are intended solely as technical support incident to the sale and use of USG products and not intended to be a substitute for the design review and approval of the licensed design professionals for the project. These materials may be printed and/or transferred electronically solely as needed by the user. Because electronic files can be modified by other parties, without notice or indication of such modifications, modification of USG Product Guide Specifications is the sole responsibility of the Design Professional.