This Guide Specification utilizes the Construction Specifications Institute (CSI) Project Resource Manual (PRM), including MasterFormat™, SectionFormat™ and PageFormat™. Specifier Notes typically precede specification text; delete notes in final copy of specification.

US MIX Co. manufacturers cementitious products and construction chemicals for the concrete construction industry including concrete, masonry mortar and grout, repair mortars, sealers, curing compounds and form releases.

This Guide Specification section specifies non-shrink, high-flow, high precision, non-metallic, non-corrosive structural cementitious-based grout.  Revise the Guide Specification section number and title below to suit project requirements, specification practices and section content. Refer to CSI MasterFormat for other section numbers and titles.

# SECTION 036000

# GROUTING

PART 1 GENERAL

  - SUMMARY

- Section includes:  Non-shrink, high precision, high-flow, non-metallic, non-corrosive cementitious-based structural grouting material.

  - RELATED SECTIONS

**NOTE TO SPECIFIER** Delete any sections below not relevant to this project; add others as required.

- Section 033000 – Cast-in-Place Concrete

- Section 034000 – Precast Concrete

- Section 05120 – Structural Steel Framing

  - REFERENCES

- ASTM International

  - ASTM C-1107 – Standard Specification for Packaged Dry, Hydraulic-Cement Grout (Non-shrink).

- International Concrete Repair Institute (ICRI)

- ICRI Technical Guideline No. 310.2R

- US Army Corps of Engineers

- CRD C-621 – Specification for Non-Shrink Grout.

1.4	SUBMITTALS

- Submit under provisions of Section 013300 – Submittal Procedures

  - Product Data:  Manufacturer’s literature to include preparation and application instructions, recommendations, storage and handling requirements.

  - Test Data:  Confirm compliance and performance with specified requirements.

1.5	QUALITY ASSURANCE

- Applicator Qualifications:  Applicator must have prior experience applying specified product or similar products, or have manufacturer’s representative on site ensuring that preparation and application are performed correctly.

- System Performance Requirements:

  - Compliance with ASTM C-1107 and CRD C-621 when tested at a fluid consistency in accordance with Manufacturer’s instructions.

- Mockup:

- A/E will select area for mockup.

- Prior notice will be given to A/E four days before mockups will be applied.

- A/E must approve mockup before final product is applied.

- At the A/E’s discretion, approved mockups may become incorporated into the final work.

- Pre-Installation Meeting:

- Convene minimum two weeks prior to starting work.  One month may be necessary when work is to be performed in cold (<40°F) or hot (>90°F) weather conditions.

  - DELIVERY, STORAGE & HANDLING

- Deliver material in original, unopened packaging with the manufacturer’s label including product name, batch number.

- Store material in a cool, dry area, above ground out of the sun.  Protect from moisture and humidity.

  - PROJECT/SITE CONDITIONS

- Environmental:  Follow Manufacturer’s instructions.  Do not apply material when temperature is below 40°F (4oC) or when expected to fall below 40°F within 48 hours.  Refer to ACI 305 “Hot Weather Concreting” and ACI 306 “Cold Weather Concreting”.

- Protection:  Precautions should be taken to avoid damage to any surface near the work zone while work is in progress until material has reached final set.

PART 2 PRODUCTS

  - MANUFACTURER

- Acceptable Manufacturer:  US MIX Co., 112 South Santa Fe Drive, Denver, CO 80223, Toll-free - 800-397-9903; Local – 303-778-7227; Fax – 303-722-8426; Web -  http://www.usspec.com.

**NOTE TO SPECIFIER** Delete one of the following two paragraphs; coordinate with requirements of Division 1 section on product options and substitutions.

- Product substitutions: Not permitted.

- Requests for substitutions will be considered in accordance with provisions of Section 016000 – Product Requirements.

  - MATERIALS

  - Non-Shrink Grout:

  - US SPEC GP Grout

  - Description:  Cement based, non-shrink, non-corrosive, non-metallic, pumpable and pourable grout.

  - Compliance:  ASTM C-1107 and CRD C-621.

  - Concrete Cleaner:

    - US SPEC Maxi Concrete Cleaner

    - Description:  Citrus-based concrete cleaner to clean and strip dirt, grease and laitance from surfaces to receive grout.

- Membrane Forming Curing Compound:

  - US SPEC Maxcure Resin Clear

  - Description:  Dissipating hydrocarbon resin curing compound.

  - Compliance:  ASTM C-309 Type I, Class B.

PART 3 EXECUTION

  - EXAMINATION

A.	Examine areas to receive grout and verify compliance with Manufacturer’s literature.  Notify Engineer if surfaces are unacceptable.  Do not begin application until unacceptable conditions are corrected.

  - SURFACE PREPARATION

- Remove all grease, oil, dirt, laitance and unsound concrete.  Smooth, dense surfaces may need to be mechanically abraded to provide necessary bonding requirements.  When necessary mechanically prepare the substrate to a minimum CSP 5 following ICRI Guideline No. 310.2R to allow proper bonding.  Substrate should be saturated, surface dry (SSD) with no standing water.  Maintain contact areas between 40°F (4°C) and 90°F (32°C) prior to application and during initial curing period.

3.3	APPLICATION

- Mix and place grout according to manufacturer’s instructions.

3.4	FINISHING

- When applicable, ensure grout “head” is at a 45 angle from bottom of plate to top of substrate.

3.5	CURING

- Place wet cloths on all exposed areas of grout for a minimum of 6 hours.

- After 6 hours, remove cloths and apply membrane forming curing compound.

3.6 PROTECTION

- Protect installed work from damage due to subsequent construction activity on site.

  - CLEAN UP

- Clean site of unused grout, waste, debris and effluent in accordance with environmental regulations.

# END OF SECTION