SECTION 030100

CONCRETE REHABILITATION

PART 1 GENERAL

  - SUMMARY

- This section specifies a rapid setting, hydraulic cement patching mortar for plugging water or other fluid leaks.

  - RELATED SECTIONS

- Section 033000 – Cast in Place Concrete

  - REFERENCES

- American Society for Testing and Materials

  - ASTM C-109 – Test Method for Compressive Strength of Hydraulic Cement Mortars Using 2 in. or 50 mm. Cube Specimens.

  - ASTM C-266 – Rate of Set with Gilmore Needle.

1.4	SUBMITTALS

- Submit under provisions of Section 013300 – Submittal Procedures

  - Product Data:  Manufacturer’s literature to include surface preparation, application instructions, recommendations and storage and handling requirements.

  - Test Data:  Confirm compliance and performance with specified requirements.

1.5	QUALITY ASSURANCE

- Applicator Qualifications:  Applicator must have prior experience applying specified product or similar products, or have manufacturer’s representative on site ensuring that preparation and application are performed correctly.

- Mockup:

  - Architect will select area for mockup.

2.	Prior notice will be given to architect four days before mockups will be applied.

3.	Architect must approve mockup before final product is applied.

4.	At the architect’s discretion, approved mockups may become incorporated into the final work.

  - DELIVERY, STORAGE & HANDLING

- Materials must be delivered in original, unopened containers with the manufacturer’s labels including product name and batch numbers.

- Store material in a dry area, above ground.  Protect cement from moisture and humidity.

  - ENVIRONMENTAL REQUIREMENTS

- Environmental Conditions:  Do not apply material when temperature is below 45°F (7oC) or when temperature is expected to fall below 45°F within 48 hours.

- Protection:  Precautions should be taken to avoid damage to any surface near the work zone.

PART 2 PRODUCTS

2.1	MANUFACTURER

- Acceptable Manufacturer:  US MIX Co., 112 South Santa Fe Drive, Denver, CO 80223, 800-397-9903, http://www.usspec.com.

2.2	MATERIALS

- Cement-Based Rapid Setting Repair Mortar:

  - US SPEC Hydraulic Cement

  - Description:  High strength, rapid hardening hydraulic cement patching mortar for stopping leaks.

  - Concrete Cleaner:

    - US SPEC Maxi Concrete Cleaner

    - Description:  Citrus-based concrete cleaner to clean and strip dirt, grease and laitance from surfaces to receive patching compound.

2.3	MATERIAL PROPERTIES

- ASTM C-109 – Compressive Strength:

  - 1 Day – 4,200 psi (28.9 MPa) minimum

  - 3 Days – 4,300 psi (29.6 MPa) minimum

  - 7 Days – 4,500 psi (31.0 MPa) minimum

  - 28 Days – 6,100 psi (42.0 MPa) minimum

- ASTM C-266 – Rate of Set:

  - Initial Set – 3 minutes minimum

  - Final Set – 5 minutes minimum, 7 minutes maximum

PART 3 EXECUTION

3.1	EXAMINATION

A.	Examine areas to be repaired.  Notify Engineer if surfaces are unacceptable.  Do not begin surface preparation or application until unacceptable conditions are corrected.

3.2	SURFACE PREPARATION

- Areas to be repaired must be clean, sound, and free of dirt, oil, grease, laitance and other contaminants.  Clean concrete with citrus-based concrete cleaner and stripper specified in Section 2.2 Materials to remove grease.  All loose and deteriorated concrete shall be removed.  Small cracks should be enlarged to maximize bonding area.

- Substrate to receive patching mortar should be saturated surface dry (SSD) per ACI recommendations.

3.3	MIXING

- Mix in an appropriate sized mechanical mixer or mix in a bucket using a drill and paddle mixer at low speed (400-600 RPM).  First, pour water into the mixing container.  Then, add powder material while continuing to mix.  Mix to a uniform consistency for a minimum of three minutes and a maximum of five minutes.

- Mix only the amount of material that can be placed within working time.  Do not re-temper material.

- Do not blend in excess liquid.  Do not use any other admixtures or additives.

3.4	APPLICATION

A.	Mortar must be placed immediately upon completion of mixing.

B.	Force material into the area to be repaired by hand or with a trowel.  To stop running water, mold by hand into a ball or wedge shape and hold in hand until material becomes warm.  Then, press firmly into opening and maintain pressure on the patch until material stops leak or approximately 3-5 minutes.  Trowel material into final shape without damaging plug.

C.	When material has reached proper set, shave, shape or mold with a steel trowel.

3.5	FINISHING

- Finish material with a broom finish or other desired finish.

3.6	CURING

A.	Cure freshly placed mortar with a liquid membrane forming curing compound.

3.7	PROTECTION

A.	Protect horizontal surfaces from traffic until repair mortar compound has cured.

# END OF SECTION