GUIDE SPECIFICATION FOR INTRAGUARD™:

CONCRETE & MASONRY WATER REPELLENT

SECTION 03 35 00

CONCRETE FINISHING

Specifier Notes: This guide specification is written according to the Construction Specifications Institute (CSI) format. The section must be carefully reviewed and edited by the architect or engineer to meet the requirements of the project. Coordinate this section with other specification sections and the drawings.

Specifier Notes: INTRAGUARD is a water-based, penetrating sealing compound for exterior concrete and masonry surfaces. Specifically designed to limit the intrusion of moisture and chlorides into the substrate, this proprietary blend of silane and siloxane penetrates into the pores of the concrete and masonry to help protect the surface from scaling caused by de-icing salts as well as protecting vertical masonry surfaces from the ingress of water. INTRAGUARD weatherproofs and protects virtually all concrete and masonry surfaces, including driveways, masonry, walkways, and vertical walls. The product is designed to provide lasting protection from de-icing chemicals and moisture intrusion. The product can be used on both horizontal and vertical surfaces. Suitable application include architectural concrete, concrete block, split-face block, pavers, stucco, porous and dense brick, clay tile, and exposed aggregate concrete.

PART 1 GENERAL

1.01	SECTION INCLUDES

A.	Surface preparation.

B.	Application of a colorless, liquid-applied, concrete and masonry water repellent.

1.02	RELATED SECTIONS

Specifier Notes: Edit the list of related sections as required for the project. List other sections dealing with work directly related to this section.

A.	Section 03 30 00 – Cast-in-Place Concrete.

B.	Section 04 20 00 – Unit Masonry.

C. 	Section 07 90 00 – Joint Sealants.

1.03		SUBMITTALS

A.	Comply with Section 01 33 00 - Submittal Procedures.

B.	Submit manufacturer's product data and application instructions.

1.04		DELIVERY, STORAGE, AND HANDLING

A.	Deliver materials to site in manufacturer's original, unopened containers and packaging, with 	labels clearly identifying product name and manufacturer.

B.	Store materials in a clean, dry area in accordance with manufacturer's instructions.

C.	Keep materials away from heat and open flame.

D.	Protect materials during handling and application to prevent damage or contamination.

1.05		ENVIRONMENTAL REQUIREMENTS

A.	Do not apply water repellent when air or surface temperatures are at a temperature of less than 40o F (4o C).

B.	Prevent from being spilled or over sprayed onto nearby water sources.

PART 2	 PRODUCTS

2.01	MANUFACTURER

A.	W. R. MEADOWS®, INC., PO Box 338, Hampshire, Illinois 60140-0338. (800) 342-5976. (847) 683-4500. Fax (847) 683-4544. Website: www.wrmeadows.com.

2.02	MATERIALS

A.	Water Repellent Coating: a water-based, penetrating sealing compound consisting of a blend of silane and siloxane.

1.	Performance Based Specification:  Water repellent coating shall have the following properties:

a.	Drying Time:  1 - 2 hours @ 70o F (21o C)

b.	VOC:  55 g/L

2. 	 Proprietary Based Specification:

a.	INTRAGUARD by W. R. MEADOWS.

PART 3 EXECUTION

3.01	EXAMINATION

A.	Examine surfaces to receive water repellent. Notify architect if surfaces are not acceptable. Do not begin surface preparation or application until unacceptable conditions have been corrected.

3.02	SURFACE PREPARATION

A.	Protect adjacent surfaces not designated to receive water repellent.

B. 	Clean and prepare surfaces to receive water repellent in accordance with manufacturer's 			instructions.

C.	Do not apply water repellent to surfaces unacceptable to manufacturer.

D. 	Ensure surfaces are structurally sound, clean and free from dirt, bitumen, efflorescence, oil, curing compounds, form oil, and other foreign matter.

E.	Apply water repellent in a test area to observe product characteristics, as temporary darkening of some substrate surfaces may occur.

F. 	Check masonry joints and repoint where necessary.

G.	Ensure all wall and roof flashings, caulking, and sealants are in good condition.

H.	Do not apply water repellent to surfaces that are to receive caulks, sealants, or any later treatment.

I.	Concrete surfaces must be fully cured and thoroughly dry prior to application.

J.	Ensure new concrete and precast panels employing type 10 cement have dried for minimum of seven days before application of water repellent.

3.03	APPLICATION

Specifier Notes: Due to porosity, certain stone and block applications may require a significant increase in coverage rate or additional applications may be necessary. Always apply a test area to determine actual coverage rate. Coverage rate will vary greatly due to the porosity of the substrate.  For optimum results, wait 14 - 28 days before applying INTRAGUARD to new concrete and masonry.

A.	Agitate material thoroughly prior to application.

B.	Apply water repellent using a low pressure sprayer with a 0.1 GPM (0.379 LPM) spray nozzle.

1.	Horizontal Application Instructions

a.	Saturate in a single application at a coverage rate of 50 - 250 ft.2/gal. (1.2 - 				6.1 m2/L).

b.	Use enough to completely wet the surface without producing puddles.  
			c.	Remove excess water repellent from the surface after 10 - 15 minutes.

2.	Vertical Applications Instructions
			a.	Apply to a visibly dry and absorbent surface at a coverage rate of 50 - 250 				ft.2/gal. (1.2 - 6.1 m2/L)

b.	Saturate from the bottom up, creating a 10" - 12" (254 mm - 305 mm) 			rundown below the spray contact point.

c.	Let the first application penetrate for 3 - 5 minutes.

d.	Re-saturate while surface is still wet.

3.04	CLEAN UP

A.	Clean equipment with mineral spirits after use.

B.	Remove overspray from glass or metal surfaces as soon as possible with mineral spirits.

END OF SECTION